GUIDE SPECIFICATION

SECTION 099723

HIGH-PERFORMANCE COATING – POLYURETHANE SEALER

PART 1 GENERAL

- SUMMARY

  - This Section specifies an applied top coat sealer for horizontal cast-in-place concrete surfaces.

  - Related Sections:

    - Section 033000 – Cast-In-Place Concrete

- SUBMITALS

  - Product Data: Submit manufacturer’s technical product data and installation instructions.

  - Mock-up: Prepare a test area minimum two feet by two feet to verify suitability of the sealer and final appearance.

- QUALITY ASSURANCE

  - Manufacturer: Minimum 20 years experience producing concrete coatings.

  - Installer: Licensed installers experience and trained in the use of high-performance top coat sealers.

  - Suitability of Substrate: Concrete must be cured, firm and dry. Surface should be clean and free of dust, oil, grease, wax, loose paint, efflorescence, rust, loose debris, or other foreign substances that may inhibit the bond between the high-performance coating and the concrete surface. A thorough pressure wash is highly recommended.

  - Regulatory Requirements: Comply with requirements of authorities having jurisdiction and application codes at the location of the project.

- DELIVERY, STORAGE AND HANDLING

  - Deliver materials and products in unopened factory labeled packages. Protect from damage.

  - Store in a safe, dry place that is out of sunlight. Keep containers tightly sealed. Do not allow product to freeze. Use within manufacturer’s recommended shelf life, approximately 12 months.

PART 2 – PRODUCTS

2.1 	MATERIALS

- Concrete Sealer: High-performance, non-yellowing, clear aliphatic polyurethane sealer with or without the use of toxic isocyanates by NewLook International, Inc., 1525 S Gladiola Street, Suite 8, Salt Lake City, UT 84104; (801) 886-9495, www.getnewlook.com. Provide the following:

- Clear Primer: NewLook PermiPrime™

- Sealer with high gloss finish: NewLook PermiPlate™

    - Performace: Concrete sealers shall meet or exceed the following requirements:

      - VOC Content: less than 2.8 lbs/gallon

      - Coverage: 300-400 square feet per mixed gallon at 2 mils DFT (no loss factor);

      - Solids content: 73% by weight, 64-65% by volume;

      - Cure time at 77 degrees Fahrenheit and 50% relative humidity at mils wet:

        - To touch: 2-3 hours;

        - Dry hard: 24 hours;

        - Full cure: 7 days;

- Self-priming sealer with high gloss finish: PermiPlate™ 0IS

    - Performance: Concrete sealer shall meet or exceed the following requirements:

      - Contains zero (0) isocyanates;

      - Contains zero (0) VOC content (VOC 0 g/L);

      - UV Stability after 3 months of simulated light exposure:

      - Coverage: 300-400 square feet per mixed gallon at 2 mils DFT (no loss factor)

      - Chemical resistance: 30-50% increase over low-grade polyurethane sealers;

PART 3 – EXECUTION

3.1 	PREPARATION

- Inspection: Prior to start of application, inspect existing conditions to ensure surfaces are suitable for installation including the following:

  - Concrete has cured for a minimum of 28 days prior to application of sealer.

  - Concrete surface must be cured, firm and dry. Surface should be clean and free of dust, oil, grease, wax, loose paint, efflorescence, rust, loose debris, or other foreign substances that may inhibit the bond between the high-performance coating and the concrete surface. A thorough pressure wash is highly recommended.

  - Concrete has been swept clean.

  - Test area has been approved.

3.2  	APPLICATION

- Concrete Sealer: Strictly comply with manufacturer’s installation recommendations as indicated by the respective technical data sheet, including the following:

- Apply after concrete or initial concrete stain coating has dried at rate recommended by manufacturer.

- Clean surface as recommended by manufacturer.

- All concrete flatwork designated as being sealed in the plans and specifications shall be sealed with 2 to 3 eave coats of sealer, at the rate of approximately 300 to 400 square feet per mixed gallon at approximately 2 mils thickness.

3.3  CLEANING AND PROTECTION

- Protection: Do not cover, but protect floor are from paint and other contaminates that could inhibit sealer from performing.

- Maintenance: Clean sealer on a regular using a concrete cleaner.

END OF SECTION